[image: image1.png]Vandagraph
>ensor Technologies






Datasheet – Gas Barrier Bag 

For Technical Diving Oxygen Sensors

	Specifications

	
	

	Part number
	0150040

	Description
	Gas barrier bag, pack of 100

	Application
	Technical diving oxygen sensors

	Size - internal
	3" x 5"

	Size - overall
	3 13/16" x 5 11/16"

	Colour
	Transparent

	Construction
	Polyolefin

	Total thickness
	4.5 mil

	Moisture Vapour Transmission Rate (ASTM F1249)
	<0.005g / 100 sq inch during 24 hrs



	Oxygen Transmission Rate 

(MOCON)
	0.15cc / 100 sq inch during 24 hrs



	Tear Strength 

(ASTM D1004-66 NOTCHED)
	MD: 5.4 lb

TD: 6.2 lb

	Tensile strength 

(ASTM D882-83, A)
	MD: 12500 psi

TD: 12500 psi

	Bursting strength 

(FTMS 191-C, 5122)
	120 psi



	Puncture strength 

(FTMS 101-C, 2065.1)
	 > 21 psi

	Heat seal strength

(ASTM D-1876-72)
	> 12 lb/in

	Light transmission 

(ASTM D1003-77)
	>90%

	Water resistance 

(FTMS 101-C, 3028, F)
	No delamination


Specifications subject to change

v1.0  10/11/10










