Oxygen sensor bags that Teledyne use

Basic 4 bags that they use are:

1) Caldry 320 - clear bags (PN B173):  material is polyethylene (for its heat-sealing property) and polyester (for its gas barrier property).  

2) CP SAT 100 - large metallic bag (B174):  same material as the clear but with inside metallic coating (for its electrostatic property).  Most widely used due to lower cost.

3) The small metallic bag (B457):  same material as the clear but with inside metallic coating. This is use as the inside bag for trace sensors.

4) The large metallic bag (A77365):  This is the same size as the B174 except it has a “Caution” statement for only trace O2 sensors. This is used as the external bag for trace sensors.

13/05/10
