
Page 1/2
SPECIFICATION

1. Type (型号): 30AWGx2C TPU JACKET
2. LHI P/N :CBX0287  REV.2 
3. Construction(结构): 

[image: image1.wmf]Shield

Outer

 

sheath

Filler

Insulation

Conductor

Wrap

250

±

10

120

±

10

14.8

±

2

Left

,Total lengh about 2.95m


4. Size and Material(线规和材料): 

	ITEM(项目)
	SPECIFICATION(标准)

	Conductor

(导体)
	Material(材料)
	Copper alloy

	
	Construction(结构)
	30AWG (25/0.05mm )

	
	Pitch (节距)
	6.35(3mm

	
	Outer diameter(外径)
	About 0.29mm

	Insulation

(绝缘)
	Material(材料)
	HDPE

	
	Average Thickness

(平均厚度)
	0.20 mm

	
	Min. Thickness

(最薄厚度)
	0.16 mm

	
	Outer diameter

(外径尺寸)
	0.69(0.05 mm

	
	Color (颜色)
	Black,White


Page 2/2
Continued
	ITEM(项目)
	STANDARD (标准)

	Filler
	Material (材料)
	Nylon

	Wrap
	Material (材料)
	PE film 

	Shield
	Material (材料)
	0.08mm Tinned copper 

	
	Type / Coverage (类型/覆盖率)
	Spiral/Min.90%

	Outer Sheath

(外护套)
	Material (材料)
	TPU 1185A

	
	Hardness (硬度)
	85A

	
	Average Thickness (平均厚度)
	0.72mm

	
	Min. Thickness(最小厚度)
	0.58mm

	
	Outer diameter (外径尺寸)
	3.3(0.10mm

	
	Color(颜色)
	Pantone yellow C

	
	Cosmetic(外观)
	Smooth (光面)


5.Properties (性能要求):
	ITEM(项目)
	SPECIFICATION(标准)

	Conductor Resistance(@20°C)

导通电阻
	376 Ohms/KM, Max.

	Dielectric Strength

高压测试
	1000V AC, 0.25mA

	Cable break force

抗拉测试
	> 20LBS

	Bending test

弯曲测试
	> 10000 cycles ±90,@200G, 60C/min, R12.5mm

	Retract ability
弹性测试
	拉到最长，在平面上自由回缩


	Revision
	Change History/ECN
	Date
	Made by
	Checked by
	Approved by

	1
	Initiation revision
	2010.06.22
	
	
	

	2
	Update 
	2010.08.13
	
	
	



_1343204271.dwg

